Chapter IV

Batteries

Coordinators:	Andreas Wiltink			SCM QM SQM SQA MC

Wen Hsin Lin			Y2Q (QRE)

WB Liu				WL1 (RD)

Barry Dai				WW0 (PM)

The two battery requirements valid so far for PHE or PHA have been retained unchanged for the current projects, respectively.

From the first common battery project a new spec will become effective. Accordingly, this section will be replaced by the new specification as soon as it has been finished and the content has been agreed with all parties concerned.

Battery requirements from PHE

1	Quality and Safety Requirements for Li-Ion Batteries used in 	BenQ’s Mobile Phones	3

1.1	Electrical conditions	3

1.1.1	Self-Discharge Current via Protection Circuit	3

1.1.2	Cycling Performance	3

1.1.3	Performance at Different Discharge Temperatures	3

1.1.4	Storage conditions	4

1.1.5	Continuous Charge	4

1.1.6	Storage, Delivery Condition	4

1.2	Mechanical and climatic conditions	5

1.2.1	Vibration Test	5

1.2.2	Shock Test	5

1.2.3	Drop Test	6

1.2.4	Temperature Range	7

1.2.5	Humidity Stress	7

1.2.6	Damp Heat Test Cyclic	7

1.2.7	Temperature Cycle Test	8

1.2.8	High Temperature Test Can type	8

1.2.9	Laminated type	9

1.2.10	Low Temperature Test	9

1.2.11	High Temperature and Humidity Test	10

1.2.12	Heat Cycle Test	10

1.2.13	Dashboard Test	10

1.2.14	Corrosion test	11

1.2.15	Heat with Sunbeam	12

1.3	Approvals	13

1.3.1	Safety Aspects/Characteristics	13

Battery requirements from PHA

SLT for batteries	14

| Test No. | Description |  |  | Standard |
| --- | --- | --- | --- | --- |
| Li-E-1 Li-E-2 Li-E-3 | # Quality and Safety Requirements for Li-Ion Batteries used in BenQ’s Mobile Phones ## Electrical conditions ### Self-Discharge Current via Protection Circuit The current consumption of the protection circuit at U_cell <= 4,2V and ambient temperature = 25°C has to be smaller than 10µA. ### Cycling Performance Conditions: Ambient temperature 20 -25°C Charge: According to charging method implemented in the mobile phone Discharge: 1C down to 3.2V Discharge capacity after 3 cycles (Cini): 100% Discharge capacity after 500 cycles: 80% ### Performance at Different Discharge Temperatures Charge and discharge conditions according to section 1.2 Methods & Conditions: Battery is fully charged at room temperature and then cooled down or heated up to the respective test temperature during a period of 15 minutes. The battery is left at this temperature for 1 hour before the discharge is started. Temp. After Cycle; -10°C; 0°C; 25°C; 60°C. 3 300 500; 40% 20% 15%; 60% 40% 30%; 100% 85% 80%; 100% 85% 75%. 100% = CINI The low temperature requirements are derived from the GSM regulations where an emergency call shall be possible. Maximum internal impedance of complete pack after 500 cycles: 160m ohm (AC). |  |
| Quantity to Test |  |  |  |  |

| Test No. | Description |  |  | Standard |
| --- | --- | --- | --- | --- |
| Li-E-4 Li-E-5 Li-E-6 | ### Storage conditions After full charge, the pack is left at 20°C for 30 days Capacity retention: 90% Capacity recovery rate (3rd cycle): 98% After full charge, the pack is left at 60°C for 30 days Capacity retention: 70% Capacity recovery rate (3rd cycle): 90%: Increase in cell thickness: according to mechanical requirements of phone After full charge, the pack is left at 45°C for 3 months Capacity retention: 70% Capacity recovery rate (3rd cycle): 90% 100% = CINI ### Continuous Charge Condition: 4,2V for 1 week Capacity retention: 97% Condition: 4,2V for 3 months (max. 0,03C rate) Capacity retention: appr. 95% Capacity recovery rate (3rd cycle): appr. 90% 100% = CINI ### Storage, Delivery Condition The battery has to be shipped in a partially charged condition, in order to enable storage of the complete battery pack for at least 1 year ex manufacturer without any charging. (Voltage ex manufacturer: OCV >= 3,7 V, after 1 year >= 3,2 V, capacity recovery rate (3rd cycle) > 90%.) 1,5 years is expected. 100% = CMIN |  |  |  |
| Quantity to Test |  |  |  |  |

| Test No. | Description |  |  | Standard |
| --- | --- | --- | --- | --- |
| Li-MC-1 Li-MC-2 | ## Mechanical and climatic conditions ### Vibration Test Vibration, sinusoidal; test according to IEC 60068-2-6. x, y, z axes (x = longitudinal axis). For each axis, new specimen must be used. Frequency range: 10 - 20 Hz Amplitude of deflection: 3.1 mm Frequency range: 20...500 Hz Amplitude of acceleration: 5 g Frequency cycles per axis: 10 Cycles = 2 hours For each axis new specimen must be used. The cells are charged 4.2V. Evaluation criteria: - The battery pack must be fully functional, no cell leakage shall occur. - No change of internal impedance (10m AC) ### Shock Test Acceleration: 500 g, pulse duration: 1 ms, Number of shocks for each direction: 3 x, y, z-axes, two directions (x = longitudinal axis) For each axis, new specimen must be used. The cells are charged to 4,2V. Evaluation criteria: - The battery pack must be fully functional, no cell leakage may occur. - No change of internal impedance (10m AC) |  |  | acc. to DIN IEC 68, part 2-6 DIN IEC 68 part 2-27 |
| Quantity to Test |  |  |  |  |

| Test No. | Description |  |  | Standard |
| --- | --- | --- | --- | --- |
| Li-MC-3 | ### Drop Test Upon impact of the battery following free fall from a given height onto a specific surface, together with the mobile phone or on its own, the battery must remain fully functional. No loose parts after drop test. The device with battery and the battery alone must be electrically and mechanically full functional. Height of drop of the pack on its own: 1.00 m/1.52 m Height of drop inside phone: 1.52 m Type of surface: Concrete or steel Direction of fall (see drop order): 4 x corners (1-2, 3-4, 5-6, 7-8) 6 x sides/surfaces 8 x edges (9, 10, 11, 12) The drops are following a random order. The cells are charged to 4.2V Evaluation criteria: - The lock mechanism has to be fully functional. The housing is allowed to open but not to disintegrate, and it must be possible to close it permanently by pressing the housing together by hand. Thereafter, the battery pack must be fully functional. - No leakage of the cells - No change of internal impedance (10m) Bounce Test: The battery is placed into mobile phone and then dropped. Direction of fall (see drop order): 8 x corners 6 x sides/surfaces 12 x edges Height of drop: 0.30 m The mobile phone is switched on and should not be switched off during this operation. |  |  | DIN IEC68, Part 2-32 Test Ed |
| Quantity to Test |  |  |  |  |

| Test No. | Description |  |  | Standard |
| --- | --- | --- | --- | --- |
| Li-MC-4 Li-MC-5 Li-MC-6 | ### Temperature Range Storage after fast charge Humidity Stress Temperature range; Duration; Capacity recovery rate (3rd cycle). -20°C  +80 °C; 5 Days; 50% of CINI. -20°C  +60 °C; 1 Month; 90% of CINI. -20°C  +45 °C; 3 Months; 90% of CINI. -20°C  +30 °C (avg. 25°C); 1 Year; 70% of CINI. Relative humidity - mean annual value max. 75% On 30 days distributed over 1 year max. 85% Temporary max. 95% Temporary slight moisture condensation permissible (for max. 1 day) Evaluation criteria: - No reduced safety characteristics during exposure to humidity and full functionality after drying up. ### Damp Heat Test Cyclic Upper air temperature: 55°C Lower air temperature: 25°C Duration: 12 + 12 h Number of cycles: 6 Evaluation criteria: - No physical change; capacity recovery rate (3rd cycle): 96% of CINI | acc. VDA 4.2 acc. IEC 60068-2-30 variant 1 |
| Quantity to Test |  |  |  |  |

| Test No. | Description |  |  | Standard |
| --- | --- | --- | --- | --- |
| Li-MC-7 Li-MC-8 | ### Temperature Cycle Test Test Nb: Change of temperature with defined rate of change. The lower and upper stress temperatures are -40°C and +80°C, respectively. Rate of temperature change: 1C/min (+ 0.2C/min) Duration of exposure: 2 hours Test time per cycle: 8 hours Number of cycles: 10 Evaluation criteria: - No physical change, capacity recovery rate (3rd cycle): 75% of CINI ### High Temperature Test Can type Applies to cells and battery packs assembled in mobile phone. Condition: Cell charged to 4.2V, storage at 80C, 120 hours Evaluation criteria: - Capacity recovery rate (3rd cycle): 50% of CINI - Physical change: See in section 1.2 Condition: Cell charged to 4.2V, storage at 80C, 24 hours Evaluation criteria: - Capacity recovery rate (3rd cycle): 80% of CINI - Physical change: See in section 1.2Error: Reference source not found The battery must not explode or catch fire if tested at 80C for 500hours. |  |  | acc. IEC 60068-2-14 acc. VDA 4.2 acc. IEC 60068-2-30 variant 1 |
| Quantity to Test |  |  |  |  |

| Test No. | Description |  |  | Standard |
| --- | --- | --- | --- | --- |
| Li-MC-9 Li-MC-10 | ### Laminated type Applies to cells and battery packs assembled in mobile phone. Condition: Cell charged to 4.2V and exposed to 30 heat cycles. A heat cycle (12 hours) consists of 1 hour temperature change from 25C to 80C, 3 hours constant temperature at 80C, 1 hour temperature change form 80C to 25C, 7 hours constant temperature at 25C. Evaluation criteria: - Capacity recovery rate (3rd cycle): 50% of CINI - Physical change: See in section 1.2 Condition: Cell charged to 4.2V, storage at 80C, 24 hours Evaluation criteria: - Capacity recovery rate (3rd cycle): 80% of CINI - Physical change: See in section 1.2 The battery must not explode or catch fire if tested at 80C for 500 hrs. ### Low Temperature Test Condition: Cell charged to 4.2V, storage at -40C, 72 hours Evaluation criteria: - Capacity recovery rate (3rd cycle): 97% of CINI - Physical change: See in section 1.2 |  |  |  |
| Quantity to Test |  |  |  |  |

| Test No. | Description |  |  | Standard |
| --- | --- | --- | --- | --- |
| Li-MC-11 Li-MC-12 Li-MC-13 | ### High Temperature and Humidity Test Condition: Cell charged to 4,2V, storage at +65°C and 90% RH for 96 hours Evaluation criteria: - Capacity recovery rate: 90% of CINI - Physical change: See in section 1.2 ### Heat Cycle Test Condition: Cell charged to 4,2V Test time at +65°C: 2 hours Test time at -25°C: 2 hours Temperature change: 2 hours Test time per cycle: 6 hours Number of cycles: 100 Evaluation criteria: - Capacity recovery rate: 85% of CINI - Physical change: S ee in section 1.2 ### Dashboard Test Condition: Cell charged to 4,2V Test time at 80°C: 6 hours Test time at 20°C 14 hours Temperature change: 2 hours Test time per cycle: 22 hours Number of cycles: 50 Evaluation criteria: - Capacity recovery rate: 50% of CINI - Physical change: See in section 1.2 |  |  |  |
| Quantity to Test |  |  |  |  |

| Test No. | Description |  |  | Standard |
| --- | --- | --- | --- | --- |
| Li-MC-14.1 Li-MC-14.2 | ### Corrosion test #### Mixed Gas test Performed according to: IEC 60068-2-60 (EN60068-2-60) Composition of gas: SO2 0,2 cm³/m³ H2S 0,01 cm³/m³ NO2 0,2 cm³/m³ Cl2 0,01 cm³/m³ Test climate: 25°C / 75% rel. humidity Test duration: 10 days Evaluation criteria: - Full functionality, no corrosion, the increase of contact resistance is max. 10 mΩ. #### Salt fog test Condition: Salt solution: 5 % NaCl (sodium chloride) Ambient temperature: pH value 6.5 - 7.2 (at 20°C ±2°C) Storage temperature: 20 °C Duration of spraying: 2 h Storage time: 22 h Number of repetitions: 1 Evaluation criteria: - Full functionality, no corrosion, the increase of contact resistance is max. 10 mΩ. |  |  | acc. IEC 60068-2-60 (EN60068-2-60) DIN EN 60068-2-52 Strength 2 |
| Quantity to Test |  |  | Quantity to Test |  |

| Test No. | Description |  |  | Standard |
| --- | --- | --- | --- | --- |
| Li-MC-15 | ### Heat with Sunbeam Performance according to IEC 60068-2-5/Sa procedure C Ambient temperature: +55C Irradiation: 1120W/m² Duration: 8 hours Evaluation criteria: - Full functionality and no physical changes of the battery pack. |  |  | acc. IEC 60068-2-5/Sa procedure C |
| Quantity to Test |  |  |  |  |

## Approvals

- UL

Applicable UL-Approval by the cell manufacturer is required. 	(presently UL 1642)

### Safety Aspects/Characteristics

Safety Characteristics for the Cell without safety circuit similar/according to UL1642 and EN60950 respective

| Test No. | Description |  |  |  |  |  | Standard |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | No. | Test Item |  | Test Conditions |  | Testing Results |  |
|  | 1 | Over Charge Test |  | Over charge is done from fully charged state by the following current (20°C) (with PTC & PCB if specified for 32V/2,5A) Voltage: max. = 32V Current: max. = 2,5A Power: max. = 48 W |  | No rupture, no fire, cell temperature max: 150°C |  |
|  | 2 | Short Circuit Test |  | Cell condition: 20°C, 4,25V |  | No rupture, no fire, cell temperature max: 125°C |  |
|  | 3 | Voltage Reversal Charge Test |  | 20°C Current: 0,9A Voltage: Max = 7,5V |  | no rupture, no fire, cell temperature max: 75°C |  |
|  | 4 | Nailing Test |  | Nail penetrates into the center part of cell through 30*48-face-wise. 1) Cell condition: charged to 4,25V. |  | No rupture, No fire, cell temperature max: 120°C |  |
|  |  |  |  | 2) Cell condition: charged to 4,40V. |  | No rupture, gas may go out, cell temperature max: 120°C |  |
|  | 5 | Cheese Cloth Test |  | According to UL 1642 |  | According to requirements of UL1642 |  |
|  | 6 | Heat Test |  | The cell is heated on a hot plate up to 165°C 1) Cell condition: charged to 4,25V |  | No rupture, no fire, leakage, cell temperature max: 165°C |  |
| Quantity to Test |  |  |  |  |  |  |  |

5. SLT for batteries

5.1 Battery SLT Test Flow

6. Activities Description

6.1 Handset SLT Test

Please refer to PA/Handset SLT test procedure(TGQA-0K-010).

  - Mechanical SLT Test

Please refer to PA/Mechanical test procedure(TGQA-0K-010).

  - Battery SLT Test

QRE Engineer will perform “Battery SLT Test” before Mass Production, and ask vendor to do the test regularly during mass production.

##### 6.3.1 Definition

##### 6.3.1.1 Samples Size

The samples need in Accessory SLT is 20 units.

6.3.1.2 Test Environment

Normal Temperature: 25°C

High Temperature: 55°C

Low Temperature: -10°C

Note : Battery charging is 0~45°C and discharging is –20C~60°C, so parametric test just  in normal temperature.

6.3.2 Parametric & Function Test

6.3.2.1 Battery

- Test Equipment :

  - Impedance Meter ( Hioki )

  - Multi-meter

  - Battery Automatic Tester (Acutech)

- Test Q’ty : 20 units

- Open Voltage Test :

| Test Condition | Measure the B- and B+ of the battery pack |
| --- | --- |
| Criteria: | Refer to SA |

- Internal Impedance Test :

| Test Condition | Measure the B- and B+ of the battery pack using the impedance meter |
| --- | --- |
| Criteria: | Refer to SA |

- Battery ID Resistance Test

| Test Condition | Measure the ID Resistance and B- of the battery pack using the multi-meter |
| --- | --- |
| Criteria: | Refer to SA |

- Battery NTC Resistance Test

| Test Condition | Measure the Thermistor and B- of the battery pack using the multi-meter |
| --- | --- |
| Criteria: | Refer to SA |

- Short Circuit Protection Test

| Test Condition | Short the B+ and B- using a short wire for one minute |
| --- | --- |
| Criteria: | Refer to SA |

- Capacity Test :

| Test Condition | Full charged then 0.5C Discharge |
| --- | --- |
| Criteria: | Refer to SA |

6.3.3 Thermal Shock Test

6.3.3.1 Test Method and Specification

-40℃~ +85℃, 45 mins/dwell@85C + 45mins/dwell@-40C/cycle

5 mins transition time, total 27 cycles

6.3.3.2 Test Q’ty : 16 units

6.3.3.3 Test Equipment

‧KSON Thermal Shock Chamber

6.3.3.4 Test Criteria

‧The products have to work normally and no mechanical material deform or crack.

6.3.4 Drop Test

6.3.4.1 Test Method and Specification

  - 120cm height natural falling to concrete floor(for battery only) , 6 faces, 1 time per face

  - 76cm height natural falling to concrete floor(for other accessories)

6.3.4.2 Test Q’ty : 16 units

6.3.4.3 Test Equipment

N/A

6.3.4.4 Test Criteria

The products have to work normally and no mechanical material deform or crack.

6.3.5 Vibration Test

6.3.5.1 Test Method and Specification

  - Frequency Range: 5Hz to 200Hz

  - Grms: 1.37G

  - Vibrate X,Y, and Z axis, 30 minutes per axis.

  - PDS versus frequency is as the below table

| Freq | PSD |
| --- | --- |
| 5 | 0.03 |
| 40 | 0.03 |
| 55 | 0.01 |
| 70 | 0.01 |
| 200 | 0.001 |

e. 	The vibration spectrum is a +3 dB / octave from 20 Hz to 80 Hz, then 0.04 g2/Hz power spectral density or at 6 g's RMS level from 80 Hz to 350 Hz, then a -3 dB / octave from 350 Hz to 2000 Hz. 3 Axis X 0.5hrs (for data cable only)

6.3.5.2 Test Q’ty : 10 units

6.3.5.3 Test Equipment

Vibration Machine

6.3.5.4 Test Criteria

a.  The products have to work normally after the test.

- Material deformation, crack, or loss is not allowed.

6.3.6 Temperature Cycling Test :

6.3.6.1 Test Procedure :

a. Battery only :

Step 1:  1hr/Dwell @-20ºC,

Step 2:  1hr. /transition from -20ºC to 65ºC

Step 3:  1hr/Dwell @65ºC,

Step 4:  1hr /transition from 65ºC to -20ºC

Repeat step 1~4; total 48hrs

b. The others :

Step 1:  1hr/Dwell @-30ºC,

Step 2:  1hr. /transition from -30ºC to 75ºC

Step 3:  1hr/Dwell @75ºC,

Step 4:  1hr /transition from 75ºC to -30ºC

Repeat step 1~4; total 48hrs

6.3.6.2 Test Q’ty : 8 units

6.3.6.3 Test Equipment	: Temp./Humid. Chamber

6.3.6.4 Test Criteria 	: The products have to work normally after the test.

6.3.7 Temperature Humidity Test

6.3.7.1 Test Procedure : Temperature/Humidity 65C/90%, total 48hrs

6.3.7.2 Test Q’ty : 8 units

6.3.7.3 Test Equipment : Temp./Humid. Chamber

6.3.7.4 Test Criteria : The product should work normally after the test.

6.3.8 ESD Test

6.3.8.1 Test Method and Specification

  - Air Discharge

Voltage: 10KV

Frequency: 1discharge/second, 10 times/point

  - Contact Discharge

Voltage: 6KV

Frequency: 1discharge/second, 10 times/point

6.3.8.2 Test Q’ty : 6 units

6.3.8.3 Test Equipment and Environment

ESD Tester at 25°C, 60%  10%RH

6.3.8.4 Test Criteria

The products have no electrical function error after the test .

6.3.9  Life Test :

Test Q’ty : 4 units

6.3.9.6 Battery

The Battery function should no reduction after insertion 3000 cycles.